## Slide 1
Investigation of MnBi-based Composite Magnets
Parashu Kharel1, Gavin Baker1, Manish Neupane1, and Tula R Paudel2
1Department of Physics, South Dakota State University, Brookings, SD 57007, USA
2 Department of Physics, South Dakota School of Mines and Technology, Rapid City, SD 57701, USA

## Slide 2
Outline
Background and Motivation
Sample preparation
Results
Conclusions

## Slide 3
Motivation and Background
High performance permanent magnetic materials are critical for modern technology including high-density recording, medical equipment, wind generators, and energy-efficient cars.
The most promising candidates of permanent magnets at present are the Dy-added Nd2Fe14B magnets.
Some promising candidates of rare-earth-free, low-cost permanent magnets: MnBi, Mn2Ga, FeNi, (Fe, Co)2B, YCo5, and HfCo7.
MnBi has a special advantage: The magnetic anisotropy increases with the increasing temperature reaching a maximum value of about 22 Mergs/cm3 at 590 K .
Low magnetization, residual Bi in the sample and poor corrosion stability of LTP phase are some issues with MnBi magnet.
Our goal is to improve the magnetization of MnBi making its composite with Fe particles.

## Slide 4
Methods
Ingots of Mn55Bi45 and Mn55Bi45Cx were synthesized using arc-melting under an argon atmosphere followed by vacuum annealing (400 °C for 8 hours).
The composite samples were made by mixing crushed powder of MnBi with commercially available Fe nanoparticles, using mortar and pastel (about 15 minutes).
The crystal structure and magnetic properties were studied using x-ray diffraction and VersaLab magnetometer.

## Slide 5
Crystal Structure
Both Mn55Bi54 and Mn55Bi45Cx samples show hexagonal NiAs-type structure (LTP).
Bi = 16 wt.%
Bi = 5 wt.%
P. Kharel et al., J. Phys. D: Appl. Phys. 55, 265003(2022).

## Slide 6
Magnetic Properties of MnBi: M(H)
Samples | M3T emu/g | (BH)max MGOe | Hc KOe | Mr/M3T (%)
Mn55Bi45Cx (Vac. annealed) Mn55Bi45Cx (Reann. in H2+Ar) | 60 57 | 7.12 7.07 | 12 17 | 97 97
Samples |  | (BH)max MGOe | Hc KOe | Mr/M3T (%)
Mn55Bi45Cx (Vac. annealed) Mn55Bi45Cx (Reann. in H2+Ar) | 60 57 | 7.12 7.07 | 12 17 | 97 97
Reannealing of MnBi powder under flow of H2 and A2 mixture has improved coercivity with little decrease in magnetization.
Reannealing: 350 oC for 1 hour
MnBi single domain diameter: ~ 0.50

## Slide 7
Magnetic Properties of MnBi and Fe: M(H)
The saturation magnetizations of composite samples are consistent with the value calculated using
Expected Coercivity:
J. Park et al., Scientific reports, 7, 4960(2017).

## Slide 8
Energy product Mn55Bi45Cx
Expected (BH)max for a magnet showing an ideal square hysteresis loop

## Slide 9
Samples | M3T (measured) emu/g | M3T(Expected) emu/g | (BH)max MGOe | Hc KOe | Mr/M3T (%)
Mn55Bi45Cx (vac. annealed) Mn55Bi45Cx (reannealed in H2+Ar) | 60 57 | - - | 7.12 (8.6)* 7.07 | 12 17 | 97 97
Fe particles | 205 | - | - | - | -
Mn55Bi45Cx +Fe (10:0.5) | 68 | 67 | 6.41 (11.1)* | 9 (10)* | 87
Mn55Bi45Cx +Fe (10:1) | 71 | 73 | 4.15 | 8.8 | 73
Mn55Bi45Cx +Fe (10:2) | 79 | 84 | - | - | -
Mn55Bi45Cx +C coated Fe (10:2) | 74 | 72 | - | - | -
Samples |  |  | (BH)max MGOe | Hc KOe | Mr/M3T (%)
Mn55Bi45Cx (vac. annealed) Mn55Bi45Cx (reannealed in H2+Ar) | 60 57 | - - | 7.12 (8.6)* 7.07 | 12 17 | 97 97
Fe particles | 205 | - | - | - | -
Mn55Bi45Cx +Fe (10:0.5) | 68 | 67 | 6.41 (11.1)* | 9 (10)* | 87
Mn55Bi45Cx +Fe (10:1) | 71 | 73 | 4.15 | 8.8 | 73
Mn55Bi45Cx +Fe (10:2) | 79 | 84 | - | - | -
Mn55Bi45Cx +C coated Fe (10:2) | 74 | 72 | - | - | -
*Expected value
Magnetic Properties: Summary

## Slide 10
Conclusions
We investigated the structural and magnetic properties of Mn55Bi45 Cx and composite of Mn55Bi45 Cx with Fe nanoparticles.
Mn55Bi45 Cx powder reannealed in a flow of Ar + H2 gas mixture shows significant increase in coercivity.
The composite of Mn55Bi45 Cx with Fe particles showed expected increase in magnetization, but the energy product was not improved due to low Mr/Ms.
The composite samples with Mn55Bi45Cx : Fe = 10:1 and with higher Fe concentration showed an indication of phase separation.
With further improvement in magnetization and squareness of hysteresis loop, it is possible to develop MnBi-based rare-earth-free permanent magnet.

## Slide 11
Thank you very much!