Investigation of MnBi-based composite magnets

Parashu Kharel1, Gavin Baker1, Manish Neupane1 and Tula R Paudel2

1Department of Physics, South Dakota State University, Brookings, SD 57007, USA

2 Department of Physics, South Dakota School of Mines and Technology, Rapid City, SD 57701, USA

Rare-earth-free permanent magnet materials have attracted much attention due to a limited supply and high price of the rare-earth metals used in current high performance magnets. MnBi and MnBi-based materials have been investigated as prospective rare-earth-free permanent magnets with moderate energy product. We have synthesized Mn55Bi45Cx magnet using arc melting and high-vacuum annealing. The composite magnets Mn55Bi45Cx-Fe and Mn55Bi45Cx-Co were prepared by grinding Mn55Bi45Cx with commercially available Fe and Co nanoparticles using mortar and pestle.  The room temperature x-ray diffraction patterns indicate that Mn55Bi45Cx crystallizes in the hexagonal NiAs-type structure. The high-field (3T) magnetization measured at room temperature for Mn55Bi45Cx is 60 emu/g and that for Mn55Bi45Cx:Fe (10:1) is 71 emu/g consistent with the theoretical prediction. The coercivity measured at 300 K for Mn55Bi45Cx and Mn55Bi45Cx:Fe  are 17 kOe and 9.0 kOe, respectively. In this presentation I will also discuss the data collected on Mn55Bi45Cx-Co samples.  (Copied from APS abstract, need modification)

- Introduction

Rare-earth-element-based permanent magnets namely Sm-Co and Nd-Fe-B developed respectively in 1960’s and 1980’s play a critical role in advancing modern technology including electrical vehicles, wind turbines, phones, refrigerators, missiles, jets etc. [1, 2]. A key characteristic that makes a permanent magnet useful is its energy product (BH)max, which depends on coercivity Hc, remanence Mr and the squareness of the hysteresis loop. Magnetization is an intrinsic property of a magnet where the upper limit of Mr is its saturation magnetization Ms, but the coercivity can be improved by optimizing its microstructure through sample processing and also by increasing the value of magnetocrystalline anisotropy energy through elemental substitution [3]. The theoretical maximum of (BH)max  for a magnet showing an ideal square hysteresis loop  is Js24 ,  where Js=4πMs. For most technological applications, a permanent magnet should retain a high value of  (BH)max  up to at least 200 oC. At present, the dysprosium containing Nd2Fe14B magnets with (BH)max of about 40 MGOe and working temperature of about 230 oC are the most promising commercial permanent magnets [4]. However, high price and issues with the supply of rare-earth elements  make them less favorable  for widespread future technological applications.  This situation has prompted a search for rare-earth-free permanent magnets.

MnBi in the hexagonal NiAs-type crystal structure is one most promising candidates of low-cost, rare-earth-free permanent magnets among several other magnets including Mn2Ga, FeNi,  Zr2Co11, YCo5, and HfCo7 [5-12]. The main advantage of MnBi is its large magnetocrystalline anisotropy, which increases with increasing temperature reaching a maximum value of  22 Mergcm-3 at 590 K. This feature is important for high temperature magnetic stability against thermal agitation [13]. However, a low saturation magnetization and high sensitivity to ambient oxygen limit its prospect for commercial application. Therefore, there have been extensive research efforts to improve its magnetic properties through suitable third element doping but the experiments have  not led to expected outcomes [7, 14, 15]. Another approach to improve its magnetic properties is to develop a hard-soft exchange coupled nanocomposite magnet using MnBi as the hard component [16,17]. Exchange coupled magnets exhibit large (BH)max utilizing high coercivity from hard phase and high magnetization from soft phase of nanocomposite. Significant improvement in (BH)max  due to exchange coupling has been demonstrated in MnBi:FeCo thin films but the thin film structures are not suitable for permanent magnet applications [18]. Our interest is to develop MnBi- based composite permanent magnet. Here, we have investigated the magnetic properties of MnBi:Fe  composite magnets.

- Experimental Methods

Mn-Bi ingots having elemental composition Mn55Bi45Cx (x < 5) were prepared using arc-melting and high-vacuum annealing. Commercially available Bi pieces, previously melted Mn and carbon power in proper weight ratio were melted together on a water-cooled Cu hearth of an arc furnace in an argon environment.  Although targeted composition was Mn55Bi45C5 , the ingot may not have that composition since some unalloyed carbon was found in the crucible after melting. We have found that Mn-Bi prepared in the presence of carbon contains less residual Bi as compared to the sample prepared without carbon [19].   The arc melted ingot was annealed in a tubular vacuum furnace (∼10−7 torr) at 400°C for 8 hours. In order to make MnBi:Fe composite, the annealed ingot was crushed into a fine powder, mixed with commercially available Fe nanoparticles, and ground in acetone for 15 minutes using mortar and pastel. We also made similar composite samples using carbon coated Fe nanoparticles.  We prepared three batches of composite samples  with Mn55Bi45Cx to Fe ratio of 20:1, 10:1 and 10:2. We call these samples Mn55Bi45Cx+Fe (20:1), Mn55Bi45Cx+Fe (10:1), and  Mn55Bi45Cx+Fe (10:2).  The crystal structures of the Mn55Bi45Cx samples were analyzed using Rigaku MiniFlex600 x-ray diffractometer with Cu-Kα source (λ = 1.54 Å), and the Quantum Design VersaLab magnetometer was used to investigate magnetic properties. The ratio of Mn and Bi in the annealed samples were confirmed using Energy-dispersive x-ray spectroscopy (EDS), which was close to the expected value within ± 1 at%.

- Results and discussion

Figure1 shows the room temperature x-ray diffraction (XRD) pattern of a powder sample prepared from the annealed Mn55Bi45Cx ingot. The XRD pattern is indexed with the hexagonal NiAs crystal structure (space group P63/mmc). This phase of MnBi is called  the low temperature phase (LTP). The inset of Fig. 1 shows the unit cell of MnBi in its LTP phase, where Mn occupies the Wyckoff’s 2a sites (0,0,0) and (0, 0, 1/2),  and Bi occupies the 2c sites (1/3, 2/3, 1/4) and (2/3, 1/3, 3/4). The interstitial sites (1/3, 2/3, 3/4) and (2/3, 1/3, 1/4) are marked I. The XRD pattern also contains peaks from residual Bi and Mn but peaks from carbon are not detected. However, the residual Bi is only about 5 wt. %. It is expected that the formation of gaseous carbon oxides during arc melting  removed impurity oxygen from the molten alloy, which increased the amount of LTP phase  reducing the amount of residual Bi in the sample [19].

.

Figure1: Room temperature x-ray diffraction pattern recorded on powder sample of Mn55Bi45Cx. Inset: Crystal structure of LTP-MnBi.

Figure 2(a) shows magnetization as a function of magnetic field of three vacuum annealed samples, namely, Mn55Bi45Cx,  Mn55Bi45Cx+Fe (20:1), and  Mn55Bi45Cx+Fe (10:1). All samples were aligned in paraffin wax at 3T before carrying out M(H) measurements. The M(H) loop of Mn55Bi45Cx+Fe (20:1) is identical to that of  Mn55Bi45Cx but there is a small kink in the M(H) loop of Mn55Bi45Cx+Fe (10:1) indicating the  weak coupling. The saturation magnetization (M3T), coercivity (Hc) and remanence ratio (Mr/M3T)  of these samples are  displayed in table 1 below. The saturation magnetizations of the composite samples are larger than that of the original Mn55Bi45Cx sample. The measured values of saturation magnetizations M3T for Mn55Bi45Cx+Fe (20:1) and  Mn55Bi45Cx+Fe (10:1) are consistent with the values calculated using M3T=M3T,sfs+M3T,hfh, where M3T,s and fs are saturation magnetization and mass fractions of soft phase [16,17]. Similar notations are used in the second term for hard phase as well. The coercivities of the composite magnets are slightly smaller than that of the original magnet (Hc =12 kOe), which are 9 kOe and 8.8 kOe for Mn55Bi45Cx+Fe (20:1) and Mn55Bi45Cx+Fe (10:1), respectively. The observed decrease in coercivity is consistent with the expectation for hard/soft composite magnets. In order to check if the magnetic properties of Mn55Bi45Cx can be improved by annealing it in hydrogen environment, the powder sample prepared for M(H)  measurement was annealed in a continuous flow of a mixture of  Hydrogen and Argon gas (10% hydrogen in Argon) at ----C. The M(H) loop measured on this sample is shown as the inset of Fig. 1. There is a significant increase in coercivity (Hc =17 kOe) with small decrease in saturation magnetization ( M3T=---).  The saturation magnetizations of Mn55Bi45Cx + Fe (10:2) and Mn55Bi45Cx + C coated Fe (10:2) composite samples are also shown in table 1. Since we saw separation of hard and soft phases in Mn55Bi45Cx+Fe (10:1), we did not  align these samples in magnetic field to find values of coercivity and remanence magnetization. The carbon coated Fe particles were  used to check the effect of interfacial carbon in magnetization. Interestingly, the measured magnetization in this sample is about 3% larger than the expected value, whereas the magnetization in similar sample made with pure Fe particles is about 6% smaller than the expected value, although the difference is within margin of error (see table 1). Theoretically, it is expected that coating MnBi grains with C enhances the magnetization [19].

Figure 2: (a) Room temperature isothermal magnetization curves M(H) of vacuum annealed Mn55Bi45Cx,  Mn55Bi45Cx+Fe (20:1), and  Mn55Bi45Cx+Fe (10:1) samples. The Inset shows the M(H) curve of Mn55Bi45Cx annealed in low hydrogen environment. (b) The BH versus H curve of vacuum annealed Mn55Bi45Cx.

Figure 2(b) shows the BH(H) curve for vacuum annealed Mn55Bi45Cx. The energy product (BH)max  determined from this curve is 7.1 MGOe. This value is  smaller than that  expected for a magnet showing an ideal square hysteresis loop (Js24=---).  Although the saturation magnetizations for composite magnets are significantly larger than that of Mn55Bi45Cx, their  energy products (BH)max are small mainly due  to small values of Mr/M3T (see table 1). We note that (BH)max   depends on  coercivity, remanence and the squareness of the hysteresis loop.

Table 1:

| Samples | M3T (measured) ±2 emu/g | M3T(Expected) ±2 emu/g | (BH)max MGOe | Hc KOe | Mr/M3T (%) |
| --- | --- | --- | --- | --- | --- |
| Mn55Bi45Cx (original) Mn55Bi45Cx (annealed in Hydrogen) | 60 | - | 7.1 | 12 17 | 97 |
| Fe particles | 205 | - | - | - | - |
| C coated Fe particles | 135 | - | - | - | - |
| Mn55Bi45Cx +Fe (10:0.5) | 68 | 67 | 6.1 | 9 | 87 |
| Mn55Bi45Cx +Fe (10:1) | 71 | 73 | 4.1 | 8.8 | 73 |
| Mn55Bi45Cx +Fe (10:2) | 79 | 84 | - | - | - |
| Mn55Bi45Cx +C coated Fe (10:2) | 74 | 72 | - | - | - |

- Conclusions

- Acknowledgments

This research is supported by South Dakota-NASA EPSCoR Research Initiation Grant no 80NSSC19M0063.

References

- F. Ronning  and S. Bader S, Rare earth repalcement magnets J. Phys.:Condens. Matter, 26, (2014), 060301.

- D. Goll, R. Loeffler, J. Herbs, R. Karimi, and G. Schneider, High-throughput search for new permanent magnet materials J. Phys.:Condens. Matter, 26, ( 2014 ) 064208.

- R. Skomski, J. M. D. Coey, Permanent Magnetism, Institute of Physics, Bristol 1999.

- J. M. D. Coey, Permanent magnet applications, J. Magn. Magn. Mater, 248, (2002), 441.

- W. Zhang, X. Z. Li, S. Valloppilly, R. Skomski,  J. E. Shield, D. J. Sellmyer, Magnetism of rapidly quenched rhombohedral Zr2Co11-based nanocomposites J. Phys. D: Appl. Phys. 46  (2013), 135004.

- W. Y. Zhang, P. Kharel, T. George, X. Z. Li, P. Mukherjee, S. Valloppilly, and D. J. Sellmyer Grain alignment due to magnetic-field annealing in MnBi:Bi nanocomposites, J. Phys. D: Appl. Phys. 49, (2016), 455002 .

- W. Zhang, B. Balasubramanian , P. Kharel,  S. Valloppilly, X. Z Li, L. Yue, R. Skomski, R. Pahari, and D. J. Sellmyer, High energy product of MnBi by field annealing and Sn doping APL Mater. 7, (2019), 121111.

- B. Balasubramanian, B. Das, R. Skomski, W. Y. Zhang, and D. J. Sellmyer, Novel nanostructured rare-earth-free magnetic materials with high energy products,  Adv. Mater. 25, (2013), 6090.

- Y. Huh, P. Kharel, V. R. Shah, E. Krrage, R. Skomski, J.E. shield, and D. J. Sellmyer,Magnetic and Strructural Properties of Rapidly Quenched Tetragonal Mn3-xGa Nanostructures, IE Trans. Magn. 49, (2013), 3277.

- S. Goto, H. Kura, E. Watanabe, Y. Hayashi, H. Yanagihara, Y. Shimada, M. Mizuguchi, K. Takanashi, and E. Kita, scientific reports , 7, 1(2017), 3216.

- B. Das , B. Balamurugan , Pankaj Kumar , R. Skomski , V. R. Shah , J. E. Shield , A. Kashyap , and D. J. Sellmyer, HfCo7-based rare-earth-free permanent magnet alloys, IEEE Trans. Magn. 49, (2013), 3330.

- N. Tang,  Z. Chen,  Y. Zhang , G. Hadjipanayis , F. Yang , Nanograined YCo5-based powders with high coercivity, J. Magn. Magn. Mater 219, (2000), 173.

- J. B. Yang, Y. B. Yang, X. G. Chen, X. B. Ma, J. Z. Han, Y. C. Yang,  S. Guo, A. R. Yan, Q. Z. Huang , M. M. Wu , D. F. Chen, Anisotropic nanocrystalline MnBi with high coercivity at high temperature Appl. Phys. Lett. 99, (2011), 082505

- P. Kharel , V. R. Shah , R. Skomski , J. E. Shield , and D. J. Sellmyer, Magnetism of MnBi-based nanomaterials, IEEE Trans. Magn. 49, (2013), 3318.

- T. R.  Paudel, B. Lama,  and P. Kharel, Ab initio study of alloying of MnBi to enhance the energy product  RSC Adv. 11, (2021 ), 30955.

- R. Skomski  and J.M.D. Coey, Giant energy product in nanostructured two-phase magnets, Phys. Rev. B 48, (1993), 15812.

- J. Park, Y-K. Hong, W. Lee, S-G. Kim, C. Rong, N. Poudel, J. P. Liu, C-J Choi, A Simple Analytical Model for Magnetization and Coercivity of Hard/Soft Nanocomposite Magnets, Scientific reports,  7, (2017), 4960.

- T. R. Gao, L. Fang, S. Fackler, S. Maruyama, X. H. Zhang, L. L. Wang, T. Rana, P. Manchanda, A. Kashyap, K. Janicka, A. L. Wysocki, A. T. N’Diaye, E. Arenholz, J. A. Borchers, B. J. Kirby, B. B. Maranville, K. W. Sun, M. J. Kramer, V. P. Antropov, D. D. Johnson, R. Skomski, J. Cui, and I. Takeuchi, Large energy product enhancement in perpendicularly coupled MnBi/CoFe magnetic bilayers, Phys. Rev. B 94, (2016), 060411(R).

- P. Kharel, B. Lama, M. Flesche, Z. Mehlberg, B. Lamsal, S. Valloppilly, Y. Zhou, D. J. Sellmyer and T R Paudel, Modifying magnetic properties of MnBi with carbon: an experimental and theoretical study, J. Phys. D: Appl. Phys. 55, (2022), 265003.